MICRO-TOPPING CEMENTITIOUS OVERLAYS

Division 3 Section 03530

PART 1     	GENERAL

1.01 SCOPE

A.  Work under this section shall include Polymer Modified Cementitious Overlayments applied over cast-in-place concrete surfaces as designated in contract documents. These toppings are designed for interior use only.  Semi-Self levels and repairs sub-floors from ¼” – 2” in one operation. All products and materials under this section shall be manufactured and supplied by manufacturer specified by the select architect or owner. All work under this section shall be performed in accordance with all manufacturers’ technical bulletins and shall conform to regulatory agencies(s) standards. The contractor for this work shall be trained and licensed by the product manufacturer.

1.02 SUMMARY

A. Related Sections:

1. Division 03 “Concrete” Section for concrete materials, reinforcing, concrete mixes, form work, placement, procedures, finishes, and moisture vapor testing:  New Concrete

a. Concrete slabs on or below grade shall be installed over an effective moisture vapor barrier.

b. Moisture Vapor Emission Testing shall be completed by the general contractor prior to installation to ensure moisture vapor emission meets the installation requirements of the select manufacturer.  If test results show excessive levels of moisture or the vapor emission rate is above that recommended by the manufacturer, install a recommended vapor emission control material as per directions.

c. Concrete slabs shall be cured 30 days and be structurally sound

d. Surface shall be straight and level with the permissible degree of tolerance of 1/4” in 10’-0” in any direction

B. Related Documents:

1.  Drawings and general provisions of the Contract, including Division 1- General Requirements, apply to this Section.

2.  Related work includes sections 03300,03360,09980,09960.

3.  Manufacturer’s technical data sheets for each product used; including all applicable instructions and installation requirements and recommendations.

1.03 SUBMITTALS

A. Submit each item in this article according to the conditions of the Contract and General Requirements Division 1 Specification Section.

B. Upon notice to proceed by an authorized individual, a sample of the concrete finish, texture and pattern, approximately 18” by 18” in the same thickness as final product, matching quality of finishing, colors, and textures to the design reference sample(s). Where finishes involve normal color and texture variations, include sample sets showing the full range of variations expected. Note: Site conditions including temperature and humidity will affect final appearance. Samples shall be completely cured and sealed as intended to approve final appearance and durability.

C. Shop drawings showing control joint and expansion joint placement, color designations keyed into the submitted control colors and accent pieces/inserts.  Drawings shall be based upon field verification of existing dimensions and conditions. Drawings shall be at a scale of at least 1/8” = 1’-0”. Enlarged plans shall be submitted for accent areas or logo detail work.

D. Submit product data, literature and Material Safety Data Sheets (MSDS) for materials to be used.  Submit Specified product data for coloring pigments, staining chemicals, sealers, etc. as proposed for the floor application.

E. Submit scaled shop drawings and graphic images as proposed in the construction drawings for review and approval by Architect and Owner or receive written approval of an on site layout before commencing work.

F. Submit certification letter stating that all materials used in conjunction with the final product conform to material regulations for installation jurisdiction.

1.04 QUALITY ASSURANCE

A. Installer Qualifications; Engage an experienced and trained installer having a minimum three (3) years documented experience who has completed special concrete finishes, similar in material, design, and extent to that indicated for this project and with a record of successful in-service performance.

B. Submit documented experience with reference letter stating project, address and contact of five (5) jobs of similar size and complexity.

C. Regulatory Requirements: Comply with provisions of air-pollution regulations of authorities having jurisdiction, including volatile organic compound regulations.

D. Samples:  Obtain Architect’s and Owner’s written approval of samples before starting the project.  Retain and maintain samples during construction in an undisturbed condition as a standard for judging the completed work.

1.05 PRE-INSTALLATION CONFERENCE

A. At least 2 weeks before, conduct conference at project site to comply with requirement of Division 1 Section "Project Meetings" and the following:

1. Review requirements for submittals, status of coordinating work, and availability of materials. Establish a preliminary progress schedule and procedures for materials inspection, testing, and certifications. Require representatives of each entity directly concerned with special concrete finishes existing substrate to attend a pre-construction conference, including, but not limited to, the following:

a. Contractor's superintendent or project manager

b. Representative from the installation crew.

c. Architect or Designer representative.

d. Owner's representative

1.06 DELIVERY, STORAGE, AND HANDLING

A. Delivery: Deliver and store packaged materials in original containers with seals unbroken and labels intact until the time of use.

B. Storage and Protection: Prevent damage of contamination of materials by water, freezing, foreign matter or other causes.

C. Provide heated and dry storage facilities on site. In addition, protect adjacent surfaces from staining and damage by covering them with impermeable coverings secured in place.

1.07 PROJECT CONDITIONS

A. Environmental Requirements:  Maintain environmental conditions and protect work during and after installation to comply with manufacturer’s printed recommendations. Maintain surface and ambient temperatures at or not less than 55 ˚F (10˚C) during installation and for 7 days after completion.  Maximum surface and ambient temperatures during application should be 85 ˚ F (30 ˚ C).  Applications made during temperatures greater than 85 ˚ F should follow Hot Weather Application Guidelines, as per ACI (American Concrete Institute)

1.08 SEQUENCING AND SCHEDULING

A. Allow sufficient time for the installation of the flooring system.  At no time shall the speed of the project completion be allowed to detrimentally effect the application.

B. Sequence topping surface, applying surface staining, antiquing, and / or surface coloring, so adjoining pours of separate times are compatible to avoid mismatching of stain or color appearances.

C. If the above is unavoidable, sequence topping surface coloring so as a minimum amount of time elapses between pours as recommended by manufacturer and approved by the Architect. Perform the topping surface staining, antiquing, and/or surface coloring in as continuous an operation as possible, utilizing same work crew to maintain continuity of finish on each surface or area of work.

E. Installation areas must be kept free from traffic and other trades during the complete application procedure and cure times.

1.09 WARRANTY

A. Manufacturer shall guarantee that all materials are free from defects and comply with published specifications and product literature.

B. Applicator shall warranty against faulty workmanship for a period of 1 year from substantial completion of the project.  Any variation of the warranty must be agreed upon and must be in writing no later than substantial completion date.

PART 2  	PRODUCTS

2.01 MATERIALS

A. Materials shall be furnished through a reputable vendor with minimum of 10 years experience with these systems.

B. Surface preparation materials: Specified Surface Cleaner, or Surface Degreaser As recommended by the select product vendor.

C. Approved Crack Repair Materials:

D. Approved Patching, Ramping, Materials

E. Approved Primers – for use over absorptive properly prepared concrete substrates

F. Polymer Modifier increases the lubricity. Topping Dry Mix - Troweled-on cementitious topping used in both interior and exterior applications.  Micro-Topping thickness is approximately 20 mils (thickness of a credit card).

G. Integral and/or topical coloration systems as approved by Architect during mockup or sample demonstration.

H. All materials shall be furnished, prepared, applied, cured, and stored according to Technical Data directions specified for use intended as specified herein.

I. Resurfacing material, additives, adhesives, patching materials, and grouts shall be from the same manufacturer.

PART 3 EXECUTIONS

3.01 EXAMINATION

A. Verification of Conditions:

1.  Provide sufficient hanging lights, power, heat, water and working conditions to permit proper application of the materials.

2.  Examine and test substrates and conditions, with installer present, for compliance with requirements for installation tolerances and other conditions affecting application of special concrete finishes. Do not proceed with application until unsatisfactory conditions have been corrected. Obligation to bring substrate to satisfactory tolerances is by owner unless otherwise specified in contracts or plans.

3.02 SURFACE PREPARATION

A. Protect adjacent and surrounding surfaces, finishes, and assemblies from surface preparation and installation method used.

B. The surface shall be clean and sound, free from any dust, dirt, oil, drywall mud, carpet glue, paint, curing and sealing compounds or any other loose materials or contaminants that may interfere with bonding.  Do not use sweeping compounds on concrete substrate for dust control, as the oils in the compound will act as a bond-breaker.

C. Concrete substrates shall be mechanically prepared by shotblasting, scarifying, or other engineering approved mechanical means.  Provide a minimum surface profile of at least CSP 5 in accordance with ICRI (International concrete repair institute) guidelines.

D. The surface shall be primed at least twice with the approved concrete Primer prior to the topping application. Follow all manufacturers’ instructions and mixing ratios for each application.

E. Patch or level any areas in need of repair with quick set patching and/or the same materials to be used for the finish surface. Follow manufacturer's Technical Data sheets for mixing, installation, and application instructions according to the depth of the repair. Areas that require attention on a majority of the surface are to have the system installed at least 24-48 hours in advance of final priming and installation. Take care to place over cured concrete surface(s) to prevent dissimilar cure rates, which may result in cracking.   Special surface treatment(s) may include membrane, crack repair, leveling and/or other.  Refer to all Technical Data sheets for individual product(s).

F. Where system(s) involve the use of several products, receive written approval of system before the start of installation.

3.03 INSTALLATION

A. Preparation: Follow instructions as in section 3.02 (A-F) Surface Preparation

B. Follow all mixing instructions per manufacturer’s technical data sheets for the Micro-topping product.

C. Take care to select the appropriate product based on specifications for site conditions, use, wear, coloration systems, substrate and/or surface moisture, and sealant and coating systems

D. If the approved design requires integral coloration, follow instructions as per the Technical Data Sheet, stay in accordance with standard practices.

E. Apply topping material per Specified Technical Data Sheet Note: It is the applicators’ responsibility to have in their possession the most recent Technical Data Sheets for the selected product and have every person on the installation crew familiar with the contents of same.

F. Take care to install over fully cured surfaces to prevent dissimilar cure rates, which may cause slight variations in the finished surface.

3.04 SPECIAL FINISHES: GENERAL

A. Maintain uniformity of special finishes over construction joints, unless otherwise indicated in writing by owner or architect.

B. Special Finish: Match Architect's design reference sample, identified and described as indicated.

C. Samples should be of large enough size to accurately show range of color and texture of the finished surface. Samples that are smaller than 18” by 18” are useful only for color selection and should not be taken as the representative of the finished look.  Samples are to be completed and then approved in writing by architect, owner or owners representative before commencement of installation unless otherwise agreed to in writing.

a. SPECIAL FINISHES:  COLORATION / SEALANTS and or COATINGS

A. Refer to Architectural Specification – Concrete Surface Finishing – Section 03360 available for download at www.concreteideas.com.

B. Refer to Architectural Specifications – Section 09980 Sealants and Coatings and Section 09960 Epoxy and Urethane Coatings available for download at www.concreteideas.com

3.05	GROUTING/ CONTROL JOINTS

A. After initial curing, as specified below, fill all lines and control joints as recommended by the product manufacturer.

Structural Grout: (Control Joints) Pre-blended high-strength shrinkage-compensated cementitious grout; ASTM C 1107 Grade C and COE CRD-C 621 Grade C. (section 07920)

a. Spread grout slurry over the surface with a squeegee or grout sponge, and remove the surplus grout.

b. Sponge clean with water.

B. Grouting of decorative saw cuts and control joints is optional and will be agreed to during the sample making process.

  - REPAIRS AND CLEANING

A. During the progress, and at the completion of the work, remove all trash, debris, etc. from the project site and leave the site clean and in an orderly condition.

B. Protect concrete surface(s) to ensure minimal damage during construction set up and move in.  Refer to section 3.07 for proper protection of the finished surface.

C. Touch-up, repair or replace damaged products before Substantial Completion. Repair damaged special concrete-finished surfaces to match color, texture, and uniformity of surrounding surfaces as closely as possible

3.07 PROTECTION

A. Installation areas must be kept free from traffic and other trades during the complete application procedure and cure time.

B. Protect finishes from adverse climatic conditions during application and curing.

C. All special finishes of concrete surfaces shall be protected against damage and stains until final acceptance of the Owner.

D. General Contractor must take the necessary precautions to protect concrete surface from all construction damage after the installation of the topping system.

E. Do not use plastic directly placed over the concrete surface or green housing will occur. Do not place OSB board or any other laminated board, which contains glue. The glue will react with the surface of the concrete. The suggested method of protection after the stains and sealers have been applied is as follows: Place cheap colorfast carpet that is breathable (not rubber backed) fuzzy side down or corrugated cardboard flat side down overlapping each edge. Masonite, OSB, or plywood may then be applied over the carpet or cardboard for further protection against scissor lifts, scaffolds, and other construction activity.

F. Do not apply duct tape or any other tape / adhesives directly onto topping surface.

3.07 MAINTENANCE

A. Follow all maintenance instructions and care procedures. Downloadable form for maintenance recommendations is available for download at www.concreteideas.com

B. Failure to follow these instructions and methods, as well as not keeping adequate and up to date maintenance records will void all warranties.

C. Maintenance of the complete flooring system is the sole responsibility of the owner unless otherwise agreed upon by means of a maintenance contract with the installer.

Part 4 – ACCEPTANCE

4.01 WRITTEN ACCEPTANCE

A. Contractor shall request inspection with architect/designer and owners representative and receive written approval upon

final application of coloration and surface finishes before applying sealer(s) and/or water repellant coatings. Contractor

shall correct deficiencies immediately (or in timely manner as agreed in writing by all parties) and request re-inspection

and letter of acceptance.

END OF SECTION

Important Information:

**Decorative Concrete Systems are hand crafted on site by trained applicators using a variety of techniques and artisan craftsmanship.  They are not pre-manufactured flooring systems therefore every system installation is unique and will present its own set of installation variables.

Similar in effect to natural stone products, the final outcome of these systems are designed to and may give an assortment of colors, swirls, mottling effects, blemishes, and occasional hairline cracks, natural to and desired when choosing these types of hand crafted systems.

Acid stain and Topical Dye coloration systems create custom translucent color effects, and are not designed to, and will not hide surface discoloration, blemishes, impressions, cracks, markings or other construction variables.  Variables that occur during installation are due to each unique working environment. (i.e. lighting, temperature, airflow, humidity, and, existing floor condition.)

Decorative Concrete Surfaces are striking in appearance and add to the artistic features of modern sculptures, floors, walls and accessories.

The total system design must be considered to ensure safe, long lasting, trouble free performance.  The installer of these systems does not take responsibility to determine and/or specify systems as stated above.  Function, material compatibility, adequate physical characteristics, and maintenance, are the responsibility of the selected architect, designer and ultimately the end user.

It is the end users’ responsibility to determine the suitability of these systems for their particular application and their own use.

Slip and Fall Precautions

The professional installer and the manufacturer of the chosen system recommends the use of slip-resistant aggregate in all coatings or flooring systems that may be exposed to wet, oily or greasy conditions.  These aggregates can be incorporated into the materials using different methods to achieve varying profiles and degrees of slip-resistance.  However, textured surfaces can be slippery under certain conditions.  Type of activity on the flooring surface, maintenance procedures and type of footwear may all be factors to consider when deciding on the degree of slip-resistance needed for a given area.   The professional installer, the manufacturer or their sales agents will not be responsible for injury incurred in a slip and fall situation.  It is the end users’ responsibility to provide for their own safety and to determine the suitability of these coatings for their particular application.

© 2006 The Ideas Media Group Inc.  Document courtesy of www.concreteideas.com