# Rough Screed Flooring Requirements for Cementitious Overlay Systems

All Overlay Systems over a rough screeded concrete slab offer a flat, smooth, wear surface without the need for finishing the concrete slab itself.

Slabs shall be screeded with a straightedge to bring the surface to the required finish level, with no coarse aggregate visible.

Concrete floors shall have the Specified Overlay System applied before the installation of the Specified Coloration and Sealant System specified.

NOTE:  Very Important

Do not use oil based sweeping compound on the slab to control dust.  The recommended sweeping compound consists of a water and sawdust mixture.  The use of an oil based sweeping compound can leave an oily residue on the surface of the slab, which could cause a bond breaking effect for the topping, this may void the warranty.

Our Craftsmen will work together with all customers, contractors and related subcontractor trades to ensure that the custom designed architectural and engineered flooring system lives up to all expectations.

Important Information for our customers:

**Decorative Concrete Systems are hand crafted on site by trained applicators using a variety of techniques and artisan craftsmanship.  They are not pre-manufactured flooring systems therefore every system installation is unique and will present its own set of installation variables.

Similar in effect to natural stone products, the final outcome of these systems are designed to and may give an assortment of colors, swirls, mottling effects, blemishes, and occasional hairline cracks, natural to and desired when choosing these types of hand crafted systems.

Acid stain and topical Dye coloration systems create custom translucent color effects, and are not designed to, and will not hide surface discoloration, blemishes, impressions, cracks, markings or other construction variables.  Variables that occur during installation are due to each unique working environment. (i.e. lighting, temperature, airflow, humidity, and, existing floor condition.)

Decorative Concrete Surfaces are striking in appearance and add to the artistic features of modern sculptures, floors, walls and accessories.

The total system design must be considered to ensure safe, long lasting, trouble free performance.  The installer of these systems does not take responsibility to determine and/or specify systems as stated above.  Function, material compatibility, adequate physical characteristics, and maintenance, are the responsibility of the selected architect, designer and ultimately the end user.

It is the end users’ responsibility to determine the suitability of these systems for their particular application and their own use.

Slip and Fall Precautions

Your professional installer and the manufacturer of the chosen system recommends the use of slip-resistant aggregate in all coatings or flooring systems that may be exposed to wet, oily or greasy conditions.  These aggregates can be incorporated into the materials using different methods to achieve varying profiles and degrees of slip-resistance.  However, textured surfaces can be slippery under certain conditions.  Type of activity on the flooring surface, maintenance procedures and type of footwear may all be factors to consider when deciding on the degree of slip-resistance needed for a given area.   The professional installer, the manufacturer or their sales agents will not be responsible for injury incurred in a slip and fall situation.  It is the end users’ responsibility to provide for their own safety and to determine the suitability of these coatings for their particular application.

© 2006 Document courtesy of www.concreteideas.com