ACID STAIN COLORATION AND COATING SYSTEM

QUICK SPECS FOR MIDLAND APPLIANCES SHOWROOM:

NOTE:  Comprehensive Architectural Specifications are available via download at www.concreteideas.com.  The following specs have been compressed from the original spec format for this section.

The following guidelines are designed for the project highlighted in the section Interior Self-Leveling Overlay Cementitious Overlays at http://www.concreteideas.com/technical/Complete_Systems/Interior_Floors.

- General Information:

- Related Section – Division 03 Concrete for concrete materials, reinforcing, concrete mixes, form work, placement, procedures, finishes a moisture vapor testing.

- The specified professional installer of these systems shall include all materials, tools, equipment and labor to complete the installation as specified below in System Specifications on page 2 of this document.

- The products and work shall be supplied by professional Installer having a minimum of three (3) years of experience with these systems including preparation, and application of the specified coloration system

- A jobsite sample has been submitted and approved by Owner or Owner’s Representative. Each sample shall remain intact for the duration of the project for reference. For each finish product specified, two samples, minimum size 18 x 18 inches square, represent actual product, color, and patterns.

- Submit all product data, technical literature, msds sheets, shop drawings and graphic images for review prior to installation.

- All parties involved must review the literature provided by the installer prior to construction.

- Deliver and store all products to the jobsite in original containers.  Protect and provide safe storage of all materials as per the manufacturer’s directions.

- Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results.  Do not install products under environmental conditions outside manufacturer's absolute limits.

- Allow sufficient time and requirements for the installation of the flooring system.  At no time shall the speed of the project completion be allowed to detrimentally effect the application.

- Sequence all work to maintain continuity of the full system installation.  No other trades will have access to the installation area during application or cure time.

- Applicator must warranty against faulty workmanship for a period of 1 year from the date of substantial completion.

- Prepare surface and install products as recommended by product manufacturer.  Surface Preparation as specified is done immediately prior to the included scope of work.

- Have in possession all recent technical data and installation sheets on site from the specified product manufacturer.

- Notify architect or owner of any unsatisfactory conditions or hazards before work begins.

- During process and at completion of work, remove all debris and trash from the project site.

- All special finishes of concrete surfaces shall be protected against damage and stains until final acceptance of the owner.  Craft Paper/ OSB board combination.  Do not affix any type of tape to the finished surface.

- Follow all maintenance recommendations and care instructions.  Maintenance is the responsibility of the owner unless agreed to by means of a maintenance contract.

The Following Easy Spec Sheet is provided to aid in the selection of product, coloration and sealant materials.

Please contact the professional installer for questions or to have this form filled out for your specific application.

ACID STAIN ON CONCRETE QUICK SPEC

PRODUCT SPECIFICATIONS

Recommended Floor Preparation Method: 	a. Degreaser, Scraping, Rotary Floor Scrubber (use of 80 – 100 grit screens or nylo grit pad) OR

b. Diamond Grinder for heavily soiled surfaces

Coloration:				Acid Stain:  Terracotta or equal

Seal System:				Solvent Based Acrylic Concrete Sealer  25% solids – 5 coats

Maintenance Start Up:			Acrylic Floor Finish – Start up 3 coats

Protection:  				Kraft Paper/ Wood Plank / Combination

Special Information/Notes:

________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________________

END OF SECTION

Important Information:

**Decorative Concrete Systems are hand crafted on site by trained applicators using a variety of techniques and artisan craftsmanship.  They are not pre-manufactured flooring systems therefore every system installation is unique and will present its own set of installation variables.

Similar in effect to natural stone products, the final outcome of these systems are designed to and may give an assortment of colors, swirls, mottling effects, blemishes, and occasional hairline cracks, natural to and desired when choosing these types of hand crafted systems.

Acid stain and topical Dye coloration systems create custom translucent color effects, and are not designed to, and will not hide surface discoloration, blemishes, impressions, cracks, markings or other construction variables.  Variables that occur during installation are due to each unique working environment. (i.e. lighting, temperature, airflow, humidity, and, existing floor condition.)

Decorative Concrete Surfaces are striking in appearance and add to the artistic features of modern sculptures, floors, walls and accessories.

The total system design must be considered to ensure safe, long lasting, trouble free performance.  The installer of these systems does not take responsibility to determine and/or specify systems as stated above.  Function, material compatibility, adequate physical characteristics, and maintenance, are the responsibility of the selected architect, designer and ultimately the end user.

It is the end users’ responsibility to determine the suitability of these systems for their particular application and their own use.

Slip and Fall Precautions

The professional installer and the manufacturer of the chosen system recommends the use of slip-resistant aggregate in all coatings or flooring systems that may be exposed to wet, oily or greasy conditions.  These aggregates can be incorporated into the materials using different methods to achieve varying profiles and degrees of slip-resistance.  However, textured surfaces can be slippery under certain conditions.  Type of activity on the flooring surface, maintenance procedures and type of footwear may all be factors to consider when deciding on the degree of slip-resistance needed for a given area.   The professional installer, the manufacturer or their sales agents will not be responsible for injury incurred in a slip and fall situation.  It is the end users’ responsibility to provide for their own safety and to determine the suitability of these coatings for their particular application.

© 2006 The Ideas Media Group Inc.  Document courtesy of www.concreteideas.com