SPECIAL PROVISION

FOR

DECORATIVE CONCRETE PAVING

## SECTION 02520

SECTION 02520 - DECORATIVE PORTLAND CEMENT CONCRETE PAVING

# PART 1 - GENERAL

SUMMARY

This Section includes exterior portland cement paving for Roadways, Curbs and guttersWalkways and Pavements

(Including Stamped Finishes)

Related Sections:  The following Sections contain requirements that relate to this Section:

Section 02300 "Earthwork" for subgrade preparation, grading and subbase course.

Section 07900 "Paving Joint Sealants" for joint fillers and sealants within concrete paving and at joints with adjacent

construction.

Section(s) 601, 802, 803, 902  2005, 2006 MDOT interim Standard for Construction

SUBMITTALS

Product Data:  Submit product data for proprietary materials and items, including reinforcement and forming

accessories, admixtures, joint systems, curing compounds, dry-shake finish materials, and others requested by

Architect.

Shop Drawings:  Submit shop drawings indicating joint spacing and locations.

Design Mixes:  Submit design mixes for each class of concrete.  Include revised mix proportions when

characteristics of materials, projects conditions, weather, test results, or other circumstances warrant

adjustments.

Laboratory Test Reports:  Submit two (2) copies of laboratory test reports for evaluation of concrete materials

and mix design tests.

Certificates:  Submit material certificates in lieu of material laboratory test reports when permitted by Architect.

Material certificates shall be signed by manufacturer and Contractor certifying that each material item complies

with or exceeds requirements.  Provide certification from admixture manufacturers that chloride content

complies with requirements.

Minutes:  Submit minutes of pre-installation conference.

SECTION 02520 - DECORATIVE PORTLAND CEMENT CONCRETE PAVING

QUALITY ASSURANCE

Concrete Standards:  Comply with provision of the following standards, except where more stringent

requirements are indicated.

American Concrete Institute (ACI) 301, "Specification for Structural Concrete for Buildings."

ACI 318, "Building Code Requirements for Reinforced Concrete."

ACI 330, "Guide for Design and Construction of Concrete Parking Lots."

Concrete Reinforcing Steel Institute (CRSI) "Manual of Standard Practice."

MDOT 2005, 2006 Interim Standard Specifications for Construction

Concrete Manufacturer Qualifications:  Manufacturer of ready-mixed concrete products complying with ASTM

C 94 requirements for production facilities and equipment.

Concrete Testing Service:  Engage a qualified independent testing agency to perform materials evaluation tests

and to design concrete mixes.

Field-Constructed Mockup:  Prior to installation of colored concrete and stamped concrete paving and curb

work, erect sample panels in place to further verify selections made for color and textural characteristics, under

sample submittals to represent completed concrete paving work for qualities of appearance, materials and

construction; build mock-ups to comply with the following requirements.  Cast a minimum of 8'x8' mockup to	demonstrate typical joints, surface finish, texture, color, and standard of workmanship.

When Architect determines that mockup does not meet requirements, demolish and remove it from the

site and cast another until the mockup is accepted.

Keep accepted mockup undisturbed during construction as a standard for judging completed paving.

Undamaged mockup may be incorporated into the Work.

Demolish accepted mockup and remove from site when directed by Architect.

Pre-installation Conference:  Conduct conference at Project site to comply with requirements of Division 1

Section "Project Meetings" and the following:

Before installing portland cement concrete paving, meet with representative of authorities having

jurisdiction, Owner, Architect, consultants, independent testing agency, and other concerned entities to

review requirements.  Notify participants at least 3 working days before conference.

PROJECT CONDITIONS

Traffic Control: Maintain access for vehicular and pedestrian traffic as required for other construction

activities, per state and local standards.

SECTION 02520 - DECORATIVE PORTLAND CEMENT CONCRETE PAVING

PART 2 - PRODUCTS

FORMS

Form Materials: Plywood, metal, metal-framed plywood or other acceptable panel-type materials to provide

full-depth,continuous, straight, smooth exposed surfaces.

Use flexible or curved forms for curves of a 100 -foot or less radius

REINFORCING MATERIALS

Reinforcing Bars and Tie Bars:  ASTM 615, Grade 60, deformed.

Joint Dowel Bars:  Plain steel bars, ASTM A 615, Grade 60.  Cut bars true to length with ends square and free

of burrs.

Hook Bolts:  ASTM A 307, Grade A Bolts, internally and externally threaded.  Design hook bolt joint assembly

to hold coupling against pavement form and in position during concreting operations, and to permit removal

without damage to concrete or hook bolt.

CONCRETE MATERIALS

Portland Cement:  ASTM C 150, Type I - II

Use one brand of cement throughout Project unless otherwise acceptable to Architect.

Fly Ash:  ASTM C 618, Type C.

Normal-Weight Aggregates:  ASTM C 33, Class 4, as follows.  Provide aggregates from a single source.

Maximum Aggregate Size: 3/4 inches

Do not use fine or coarse aggregates that contain substances that cause spalling.

Local aggregates not complying with ASTM C 33 that have been shown to produce concrete of

adequate strength durability by special tests or actual service may be used when acceptable to

Architect.

Fiber Reinforcement:  Synthetic fibers engineered and designed for secondary reinforcement of concrete slabs,

complying with ASTM C 1116, Type III.

ADMIXTURES

Admixtures containing chloride cannot be used

Air-Entraining Admixture:  ASTM C 260, certified by manufacturer to be compatible with other required

admixtures.

SECTION 02520 - DECORATIVE PORTLAND CEMENT CONCRETE PAVING

Water-Reducing Admixture:  ASTM C 494, Type A and containing no calcium chloride ions.

High-Range Water-Reducing Admixture:  ASTM C 494, type F or type G, and containing no calcium chloride

ions.

Water-Reducing and Accelerating Admixture:  ASTM C494, Type E.

Water-Reducing and Retarding Admixture:  ASTM C 494, Type D

CURING MATERIALS

Absorptive Cover:  Burlap cloth made from jute or kenaf, weighing approximately 9 oz. per sq. yd., complying

with AASHTO M 182, Class 2.

Moisture-Retaining Cover:  Provide either polyethylene film or a white burlap-polyethylene sheet, complying

with ASTM C 171.

Curing Compound:  ASTM C 309; Clear, liquid type membrane-forming water soluble, VOC compliant,

sprayable curing compound; submit certification of compliance from manufacturer.  (Note: Standard curing compounds will not be used on colored or decorative concrete.  See Sealer section below for approved products.)

RELATED MATERIALS

Traffic Paint:  Alkyd-resin ready-mixed, complying with ASSHTO M 248, Type S. Color:  White or Yellow as

indicated.

Decorative Concrete Color Products

Approved Manufacturers

- Prism Pigments

- Scofield Distribution

- Matcrete 913-422-4443

Concrete Integral Color: Pre-weighed and packaged dry high grade coloring pigment in either powder or granular form..

Material must comply with ASTM C-979 standards for colored concrete.  Color as indicated or approved manufacturer equal.

- Prism Pigments: ______________

Decorative Concrete Dry-Shake Color Hardener:  Packaged dry combination of materials consisting of portland cement

graded silica, coloring pigments, and plasticizing admixture.  Use coloring pigments that are finely ground

nonfading mineral oxides interground with cement.  Color as indicated below.  Recommended coverage 60lbs./100 sq.ft.

- Matcrete Dustone C/H: ________

Release Agent:  Dry-shake powder to facilitate release of imprinting tools as manufactured by Matcrete or TK Products (Liquid).  Color as indicated or approved manufacturer equal.

- Matcrete Dustone R/A Powder: _____

- Matcrete Liquid Release (or TK Products)_____

SECTION 02520 - DECORATIVE PORTLAND CEMENT CONCRETE PAVING

Sealer:  Provide “crystal clear” solvent acrylic decorative sealer from approved listing

- TK Products

  - AK2 Achro Kure 1315 Solvent base sealer (curing compound) Or

  - TK 2519 WB Dissipating Cure (If Acid Stain to be used later, use this cure)

  - TK Bright Glaze solvent base sealer (High gloss Top coat) Or

  - TK Bright Kure N Seal (Less gloss Top Coat)

Bonding Agent:  Acrylic or styrene butadiene.  Subject to compliance with requirements, provide by the color hardener 	manufacturer if required.

Epoxy Adhesives:  ASTM C 881, two-component material suitable for dry or damp surfaces.  Provide material

type, grade, and class to suit requirements.  Subject to compliance with requirements. Submit certification of

compliance from approved manufacturers or demonstrated approved equal

CONCRETE MIX

Prepare design mixes for each type and strength of normal-weight concrete by either laboratory trail batch or

field experience methods as specified in ACI 301.  For the trial batch method, use a qualified independent

testing agency for preparing and reporting proposed mix designs.

Do not use the Owner's field quality-control testing agency as the independent testing agency

Limit use of fly ash to 15 percent of cement content by weight

Proportion mixes according to ACI 211.1 and ACI 301 to provide normal-weight concrete with the following

properties:

Compressive Strength (28 Day): 4000 psi

Maximum Water-Cement Ratio at Point of Placement: 0..46

Slump Limit at Point of Placement: 4 inches minimum

Slump limit for concrete containing high-range water-reducing admixture (superplasticizer):

Not more than 8 inches after adding admixture to site-verified 4-inch slump concrete.

Add air-entraining admixture at manufacturer's prescribed rate to result in concrete at point of placement having

An air content as follows with a tolerance of plus or minus 1 1/2 percent:

Air Content:  5.5 percent for 1 1/2-inch maximum aggregate.

Air Content: 6.0 percent for 1-inch maximum aggregate.

Air Content: 6.0 percent for 3/4-inch maximum aggregate.

Air Content: 7.0 percent for 1/2-inch maximum aggregate.

Fiber Reinforcement:  Add to mix at rate of 1.5 lb per cu.yd., unless manufacturer recommends otherwise.

Adjustment to Concrete Mixes:  Mix design adjustments may be requested by Contractor when characteristics

of materials project conditions, weather, test results, or other circumstances warrant.

### CONCRETE MIXING

Ready-Mixed Concrete:  Comply with requirements and with ASTM C 94.

When air temperature is between deg F (30deg C) and 90 deg F (32 C) reduce mixing and

delivery time form 1 1/2 hours to  75 minutes' when air temperatures above 90 deg F (32 deg C),

reduce mixing and delivery time to 60 minutes.

SECTION 02520 - DECORATIVE PORTLAND CEMENT CONCRETE PAVING

IMPRINTING TOOLS

Approved Manufacturers and Patterns

Matcrete Concrete Tools

Proline Concrete Tools

Mat Tools: Tools shall be high quality resilient mats reproduced from castings of natural materials and

providing uniform control of joint depth.

Provide pattern(s) shown on Drawings and/or listed by architect or designer.  Substitute mat design must be presented to 	the Engineer for approval and must be accompanied by a sample as defined in this specification.

PART 3 - EXECUTION

PREPARATION

Lay Out:  Carefully lay out form work and joints taking into consideration pattern, intended aesthetics, and

construction sequence.  Lay out long lines of patterns to run across the normal line of sight (except where

otherwise shown on Drawings).

Surface Preparation:

Proof-roll prepared subbase surface to check for unstable areas verify need for additional compaction.  Do

not begin paving work until such conditions have been corrected and are ready to receive paving.

Remove loose material from compacted subbase surface immediately before placing concrete.

EDGE FORMS AND SCREED CONSTRUCTION

Set, brace, and secure edge forms, bulkheads, and intermediate screed guides for paving to required lines,

grades, and elevations.  Install forms to allow continuous progress of work and so that forms can remain in

place at least 24 hours after concrete placement.

Check completed formwork and screeds for grade and alignment to following tolerances:

Top of Forms:  Not more than 1/8 inch in 10 feet.

Vertical Face on Longitudinal Axis:  Not more than 1/4 inch in 10 feet

Clean forms after each use and coat with form release agent as required to ensure separation from concrete

without damage.

JOINTS

General:  Construct contraction, construction, and isolation joints true to line with faxes perpendicular to

surface plane of concrete.  Construct transverse joints at right angles to the centerline, unless indicated

otherwise.

When joining existing paving, place transverse joints to align with previously placed joints, unless

indicated otherwise.

Contraction Joints:  Provide weakened-plane contraction joints, sectioning concrete into areas as shown on

Drawings.  Construct contraction joints for a depth equal to at least 1/4 of the concrete thickness, as follows:

Tooled Joints:  Form contraction joints in fresh concrete by grooving and finishing each edge of joint

with a radiused jointer tool.

SECTION 02520 - DECORATIVE PORTLAND CEMENT CONCRETE PAVING

Sawed Joints:  Form contraction joints with power saws equipped with shatterproof abrasive or

diamond-rimmed blades.  Cut 3/8 inch-wide into hardened concrete when cutting action will not

tear, abrade, or otherwise damage surface and before development of random contraction cracks.

Inserts:  Form contraction joints by inserting premolded plastic, hardboard or fiberboard strips into

fresh concrete until top surface of strip is flush with paving surface.  Radius each joint edge with a

jointer tool.  Carefully remove strips or cans of two-piece assemblies after concrete as hardened.

Clean groove of loose debris.

Construction Joints:  Set construction joints at side and end terminations of paving and at locations where

paving operations are stopped for more than 1/2 hour, unless paving terminates at isolation joints.

Provide preformed galvanized steel or plastic keyway-section forms or bulkhead forms with keys,

unless indicated otherwise. Embed keys at least 1-1/2 inches into concrete.

Continue reinforcement across construction joints unless indicated otherwise.  Do not continue

reinforcement through side of strip paving unless indicated.

Provide tie bars at side of paving strips where indicated.

Use bonding agent on existing concrete surfaces that will be joined with fresh concrete.

Where load transfer-slip dowel devices are used install so that one end of each dowel bar is free to

move

Isolation (Expansion) Joints: Form isolation joints of preformed joint filler strips abutting concrete curbs, catch

basins, manholes, inlets, structures, walk, other fixed objects, and where indicated.

Locate expansion joints where indicated and or abutting a vertical surface

Extend joint fillers width and depth of joint not less than 1/2 inch or more than 1 inch below

finished surface where joint sealant is indicated.  Place top of joint filler flush with finished concrete

surface when no joint sealant is required.

Furnish joint fillers in one-piece lengths for full width being placed wherever possible.  Where more

than one length is required, lace or clip joint filler sections together.

Protect top edge of joint filler during concrete placement with a metal, plastic, or other temporary

preformed cap.  Remove protective cap after concrete has been placed on both sides of joint.

Installation of joint fillers and sealants is specified in Division 7 Section "Paving Joint Sealants."

Install dowel bars and support assemblies at joints where indicated.  Lubricate or asphalt-coat one half of dowel

length to prevent concrete bonding to one side of joint.

SECTION 02520 - DECORATIVE PORTLAND CEMENT CONCRETE PAVING

CONCRETE PLACEMENT

Inspection:  Before placing concrete, inspect and complete formwork installation, reinforcing steel and items to

be embedded or cast in. Notify other trades to permit installation of their work.

Remove snow, ice, or frost form subbase surface and reinforcing before placing concrete.

Do not place concrete on surfaces that are frozen.

Moisten subbase to provide a uniform dampened condition at the time concrete is placed.  Do not place

concrete around manholes or other structures until they are at the required finish elevation and alignment.

Comply with requirements and with ACI 304R for measuring, mixing, transporting, and placing concrete.

Deposit and spread concrete in a continuous operation between transverse joints.  Do not push or drag concrete

into place or use vibrators to move concrete into place.

When concrete placing is interrupted for more than 1/2 hours, place a construction joint.

Use a bonding agent at locations where fresh concrete is placed against hardened partially hardened concrete

surfaces.

Consolidate concrete by mechanical vibrating equipment supplemented by hand-spading, rodding,or tamping.

Use equipment and procedures to consolidate concrete complying with ACI 309R.

Consolidate concrete along face of forms and adjacent to transverse joints with an internal vibrator.

Keep vibrator away from joint assemblies, reinforcement, or side forms.  Use only square-faced

shovels for hand-spreading and consolidation.  Consolidate with care to prevent dislocating

reinforcing, dowels, and joint devices.

Screed paved surfaces with a straight edge and strike off.  Use bull floats or darbies to form a smooth surface

plane before excess moisture or bleed water appears on the surface.  Do not further disturb concrete surfaces

prior to beginning finishing operations.

Place concrete in two operations; strike off initial pour for entire width of placement and to the required depth

below finish surface.  Lay welded wire fabric or fabricated bar mats immediately in final position.  Place top

layer of concrete, strike off, and screed.

Remove and replace portions of bottom layer of concrete that have been placed more than 15 minutes

without being covered by top layer or use bonding agent if acceptable to Architect.

Colored Concrete:  Comply with the colored pigment/hardener manufacturer's published

recommendations and instructions for mix designs, concrete temperature, mixing, admixtures, installing,

finishing and curing.  Coordinate stamped colored concrete to ensure consistency in color, texture and quality.

Color Hardener:  Apply a minimum of 60 pounds per 100 Sq.Ft.  Apply evenly in two passes from different directions

using dry-shake method. When moisture is present bull float each application of the shake. Apply Release Agent.

Imprint Pattern:  Comply with tool manufacturer's standards.  Lay out to proper alignment and imprint a consistent depth 	while concrete is plastic.  Hand-tool in areas where imprinting tools are not practical.

Removal of Excess Powder Release:  Excess release should be washed off with normal garden hose prior to control joints 	being cut.   Power washing is not permitted.  (Note: Temperature conditions will dictate the timing of release removal.)

Disposal to be compliant with local regulations.

SECTION 02520 - DECORATIVE PORTLAND CEMENT CONCRETE PAVING

Control Joints: Provide (grooved) or (sawn) joints. In walks, locate joints at invervals not to exceed 1-1/2 width of walk

but not more than 10 ft. on center.  In large paved areas, locate not more than 12 ft. on center to form rectangles

with long dimension not more than 1-1/2 x short dimension.  Depth shall be 1/4 thickness of slab

Coordinate joint locations with layout of imprinted pattern when practical.

Protect concrete form premature drying, excessive hot or cold temperature, and damage.  Evaporation Retarder may be applied to assist in preventing premature drying.  Detailing:  After concrete has set for at least 24 hours, chisel to remove marks left by imprinting tools.  Color chipped areas with slurry of color hardener mixed with water and bonding agent.

Curbs and gutters:  When automatic machine placement is used for curb and gutter placement, submit revised

mix design and laboratory test results that meet exceed requirements.  Produce curbs and gutters to required

cross section, lines, grades, finish, and jointing as specified for formed concrete.  If results are not acceptable,

remove and replace with formed concrete.

Cold-Weather Placement: Comply with provisions of ACI 306R and as follows:  Protect concrete work form

physical damage or reduced strength that could be caused by  frost, freezing actions, or low temperatures.

When air temperature has fallen to or is expected to fall below 40 deg F (4 deg C), uniformly heat

water and aggregates before mixing to obtain a concrete temperature of not less than 50 deg F

(10deg C) and not more than 80deg F (27 deg C) at point of placement.

Do not use frozen materials or materials containing ice or snow.

Do not use calcium chloride, salt, or other materials containing antifreeze agents or chemical

accelerators unless otherwise accepted in mix designs.

Hot-Weather Placement:  Place concrete complying with ACI 305R and as specified when hot weather

conditions exist.

Cool ingredients before mixing to maintain concrete temperature of time of placement to below 90

deg F (32 deg C).  Mixing water may be chilled or chopped ice may be used to control temperature,

provided water equivalent of ice is calculated to total amount of mixing water. Using liquid nitrogen

to cool concrete is Contractor's option.

Cover reinforcing steel with water-soaked burlap if it becomes too hot, so that steel temperature will

not exceed the ambient air temperature immediately before embedding in concrete.

Fog spray forms, reinforcing steel, and subgrade just before placing concrete. Keep subgrade moisture

uniform without standing water, soft sports, or dry areas.  Evaporation Retarder shall be used on

the decorative concrete surfaces see manufacturers recommendations.

CONCRETE FINISHING

Float Finish:  Begin floating when bleed water sheen has disappeared and the concrete surface has stiffened

sufficiently to permit operations. Float surface with power-driven floats, or by hand floating if area is small or

inaccessible to power units. Finish surfaces to true planes within a tolerance of 1/4 inch in 10 feet as

determined by a 10-foot-long straightedge placed anywhere on the surface in any direction. Cut down high

spots and fill low spots. Refloat surface immediately to a uniform granular texture.

Medium-to-Fine-Textured Broom Finish:  Draw a soft bristle broom across concrete surface perpendicular to line

of traffic to provide a uniform fine texture finish in non-stamped areas.

SECTION 02520 - DECORATIVE PORTLAND CEMENT CONCRETE PAVING

Final Toolings:  Tool edges of paving, gutter, curbs, and joints formed in fresh concrete with a jointing tool to

the following radius. Repeat tooling of edges and joints after applying surface finishes.  Eliminate tool marks

on concrete surfaces.

Radius:  1/4 inch.

Acid wash Decorative Surface:  Apply a 1 part muratic acid to 10 parts potable water to the surface and agitate

with side of a straw broom a minimum of 36 hours after placement.  Wash the surface until proper color has

been achieved and then flush thoroughly. (DO NOT use muriatic acid if planning to acid stain.)

Detailing: squeeze joints are present a 4” grinder should be used to remove.  Ground areas should then be burnished

With dry release using a camel back sponge.  Blow away excess release with high velocity blower.

Seal Decorative Surfaces:  7 – 10 days after acid wash/etching technique is performed, surface is to be sealed with 	approved Decorative sealer.  (Refer to Related materials section for approved products and manufacturer tech data sheet 	for proper installation procedures.)

CONCRETE PROTECTION AND CURING

General:  Protect freshly placed concrete from premature drying and excessive cold or hot temperatures.

Comply with the recommendations of ACI 306R for cold weather protection and ACI 305R for hot weather

protection during curing.

Evaporation Control:  In hot, dry, and windy weather, protect concrete from rapid moisture loss before and

during finishing operations with an evaporation retardant..  Apply according to manufacturer's

instructions after screeding and bull floating, but before finishing.

Begin curing after finishing concrete but not before free water has disappeared from concrete surface.  This needs to be 	done the same day of the pour.

Curing Methods:  Cure concrete by moisture curing, moisture-retaining -over curing, curing compound, or a

combination of these as follows:

Moisture Curing:  Keep surfaces continuously moist for not less than 7 days with the following

materials:

Water.

Continuous water-fog spray.

Absorptive cover, water saturated, and kept continuously wet.  Cover concrete surfaces and

edges with a 12-inch lap over adjacent absorptive covers.

Moisture-Retaining-Cover Curing:  Cover concrete surfaces with moisture-retaining cover for curing

concrete, placed in widest practicable width, with sides and ends lapped at least 12 inches, and sealed

by waterproof tape or adhesive.  Immediately repair any holes or tears during curing period using

cover material and waterproof tape.

Curing Compound:  Apply uniformly in continuous operation by power spray or roller according to

manufacturer's directions.  Recoat areas subjected to heavy rainfall within 3 hours after initial

application.  Maintain continuity of coating and repair damage during curing period.

Note:  This is for standard gray Portland concrete only.  Refer to Sealing sections for proper procedures on 			colored and decorative concrete.

SECTION 02520 - DECORATIVE PORTLAND CEMENT CONCRETE PAVING

TRAFFIC PAINT

Traffic Paint:  Apply traffic paint for striping and markings with mechanical equipment to produce

uniform straight edges.  Apply at manufacturer's recommended rates to provide a 15-mil minimum wet film

thickness.

FIELD QUALITY CONTROL TESTING

Employ a qualified independent testing and inspection agency to sample materials, perform tests, and submit

test reports during concrete placement as follows:

The Owner will employ a qualified testing and inspection agency to sample materials, performs tests, and submit

test reports during concrete placement.  Sampling and testing for quality control may include the following:

Sampling Fresh Concrete:  ASTM C 172, except modified for slump to comply with ASTM C 94.

Slump:  ASTM C 143; one test a t point of placement for each compressive-strength test but

no less than one test for each day's pour of each type of concrete.  Additional tests will be

required when concrete consistency changes.

Air Content:  ASTM C 231, pressure method; one test for each compressive-strength test but

no less than one test for each day's our of each type of air-entrained concrete.

Concrete Temperature:  ASTM C 1064; one test hourly when air temperature is 40 deg F (4

deg C) and below and when 80 deg F (27 deg C) and above and one test for each set of

compressive-strength specimens.

Compression Test Specimens:  ASTM C 31; one set of four standard cylinders for each

compressive-strength test, unless directed otherwise.  Mold and store cylinders for

laboratory-cured test specimens except when field-cured test specimens are required.

Compressive-Strength Tests:  ASTM C 39; one set for each day's pours of each concrete class

exceeding 5 cu. yd. but less than 25  cu. yd., plus one set for each additional 50 cu. yd. Test

one specimen at 7 days, test two specimens at 28 days, and retain one specimen in reserve for

later testing if required.

When frequency of testing will provide fewer than five strength tests for a given class of concrete,

conduct testing from at least five randomly selected batches or from each batch if fewer than five are

used.

When total quantity of a given class of concrete is less than 50 cu. yd., Architect may waive strength

testing if adequate evidence of satisfactory strength is provided.

When strength of field-cured cylinders is less than 85 percent of companion laboratory-cured

cylinders, evaluate current operations and provide corrective procedures for protecting and curing the

in-place concrete.

Strength level of concrete will be considered satisfactory if averages of sets of three consecutive

strength test results equal or exceed specified compressive strength and no individual strength test

result falls below specified compressive strength by more than 500 psi.

SECTION 02520 - DECORATIVE PORTLAND CEMENT CONCRETE PAVING

Test results will be reported in writing to Architect, concrete manufacturer, and Contractor within 24 hours of

testing.  Reports of compressive strength tests shall contain the Project identification name and number, date of

concrete placement, name of concrete testing agency, concrete type and class, location of concrete batch in

paving, design compressive strength at 28 days, concrete mix proportions and materials, compressive breaking

strength, and type of break for both 7-day and 28-day tests.

Nondestructive Testing:  Impact hammer, sonoscope, or other nondestructive device may be permitted by shall

not be used as the sole basis for acceptance or rejection.

Additional Tests:  The testing agency will make additional tests of the concrete when test results indicate slump,

air entrainment, concrete strengths, or other requirements have not been met, as directed by Architect. Testing

agency may conduct tests to determine adequacy of concrete by cored cylinders complying with ASTM C 42,

or by other methods as directed.

REPAIRS AND PROTECTION

Remove and replace concrete paving that is broken, damaged, or defective, or does not meet the requirements

of this Section.

Drill test cores where directed by Architect when necessary to determine magnitude of cracks or defective

areas.  Fill drilled core holes in satisfactory pavement areas with portland cement concrete bonded to paving

with epoxy adhesive.

Protect concrete from damage.  Exclude traffic from paving for at least 14 days after placement.  When

construction traffic is permitted, maintain paving as clean as possible by removing surface stains and spillage of

materials as they occur.

Maintain decorative concrete paving free of stains, discolorations, dirt, and other foreign material.  Sweep and wash

concrete paving not more than 2 days prior to date scheduled for Substantial Completion inspections.

Away and clean potable water.

Remove all hard water stains (white chalky build up) from the top of the sealer surface, with commercial grade Lime

END OF SECTION 02520